# G2 Clean Slab Structures — Initial (POSCAR)

Pd/PdO/PdO₂ DMC Study  |  Initial Structures  |  POV-Ray -75x,15y,3z

| S1: Pd(100) Metallic Pd, p(4×4), 4 layers CONVERGED | S2: PdO(101)/Pd(100) (√5×√5)R27° surface oxide on Pd(100), 2×2 RUNNING |
| --- | --- |
| S3: PdO(100) Bulk PdO, O-rich termination, 4×2 CONVERGED | S4: PdO₂(110) Rutile PdO₂, stoichiometric termination RUNNING |

## Slab Properties (Initial Structure)

| Surface | Oxidation | Atoms | Pd / O | Cell a × b (Å) | Layers | Fixed | Status |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S1: Pd(100) | Pd⁰ | 80 | 80 / 0 | 11.0 × 11.0 | 5 | 32 | CONVERGED |
| S2: PdO(101)/Pd(100) | Pd⁰/Pd²⁺ | 112 | 96 / 16 | 12.3 × 12.3 | 7 | 40 | RUNNING |
| S3: PdO(100) | Pd²⁺ | 128 | 64 / 64 | 12.2 × 10.8 | 8 | 32 | CONVERGED |
| S4: PdO₂(110) | Pd⁴⁺ | 144 | 48 / 96 | 9.5 × 12.8 | 16 | 45 | RUNNING |

## Layer Structure Detail

S1: Pd(100)

| Layer | z (Å) | Pd | O | Constraint |
| --- | --- | --- | --- | --- |
| 1 | 1.50 | 16 | - | FIXED |
| 2 | 3.45 | 16 | - | FIXED |
| 3 | 5.39 | 16 | - | free |
| 4 | 7.34 | 16 | - | free |
| 5 | 9.28 | 16 | - | free |

S2: PdO(101)/Pd(100)

| Layer | z (Å) | Pd | O | Constraint |
| --- | --- | --- | --- | --- |
| 1 | 1.50 | 20 | - | FIXED |
| 2 | 3.45 | 20 | - | FIXED |
| 3 | 5.39 | 20 | - | free |
| 4 | 7.34 | 20 | - | free |
| 5 | 9.54 | 16 | - | free |
| 6 | 10.20 | - | 8 | free |
| 7 | 11.53 | - | 8 | free |

S3: PdO(100)

| Layer | z (Å) | Pd | O | Constraint |
| --- | --- | --- | --- | --- |
| 1 | 1.50 | 8 | - | FIXED |
| 2 | 3.03 | 8 | 16 | FIXED |
| 3 | 4.57 | 8 | - | free |
| 4 | 6.12 | 8 | 16 | free |
| 5 | 7.65 | 8 | - | free |
| 6 | 9.14 | 8 | 16 | free |
| 7 | 10.75 | 8 | - | free |
| 8 | 12.05 | 8 | 16 | free |

S4: PdO₂(110)

| Layer | z (Å) | Pd | O | Constraint |
| --- | --- | --- | --- | --- |
| 1 | 1.84 | - | 9 | FIXED |
| 2 | 2.53 | - | 3 | FIXED |
| 3 | 3.55 | 12 | 9 | FIXED |
| 4 | 4.21 | 3 | 9 | FIXED |
| 5 | 5.21 | - | 6 | FIXED |
| 6 | 6.41 | 6 | 6 | free |
| 7 | 7.22 | 6 | 9 | free |
| 8 | 7.91 | - | 3 | free |
| 9 | 8.69 | - | 6 | free |
| 10 | 9.92 | 6 | 9 | free |
| 11 | 10.60 | 6 | 6 | free |
| 12 | 11.37 | - | 3 | free |
| 13 | 11.93 | - | 6 | free |
| 14 | 12.47 | - | 3 | free |
| 15 | 13.40 | 9 | 9 | free |
| 16 | 14.02 | 3 | 3 | free |

## Construction Notes

S1: Pd(100)

ase.build.fcc100, a = 3.891 Å from G1 bulk Pd

p(4×4), 4 layers, 20 Å asymmetric vacuum, bottom 2 fixed

CONVERGED: max force (free) = 0.019 eV/Å, E = −434.408 eV

S2: PdO(101)/Pd(100)

√5×√5 R27° surface oxide monolayer on Pd(100) substrate

Oxide: pymatgen SlabGenerator(PdO, (1,0,1)) → 3D rotation to flat → 2×1 supercell

Strain: PdO(101) 2×1 (6.11×6.21 Å) → √5×√5 Pd(100) (6.15×6.15 Å), < 1%

Intra-oxide Pd–O: 2.02–2.04 Å (bulk PdO: 2.039 Å) — correct geometry

Oxide orientation: Pd at interface, O at surface (flipped to match experiment)

2×2 final supercell → 112 atoms (80 sub + 16 Pdₒₓ + 16 O)

S3: PdO(100)

pymatgen SlabGenerator(PdO, (1,0,0)), O-rich termination, 4×2 supercell

CONVERGED: max force (free) = 0.023 eV/Å, E = −724.152 eV

S4: PdO₂(110)

pymatgen SlabGenerator(PdO₂, (1,1,0)), stoichiometric termination

Rutile-type PdO₂, Pd⁴⁺ oxidation state

## VASP Settings

ENCUT = 520 eV, PREC = Accurate, ISPIN = 2, IVDW = 12 (D3-BJ)

EDIFF = 1e-6, EDIFFG = −0.03 eV/Å, IBRION = 2, NSW = 300, ISIF = 2

KSPACING = 0.25, LDIPOL = T, IDIPOL = 3, ISYM = 0

S1: ISMEAR=1, SIGMA=0.1 (metal) | S2–S4: ISMEAR=0, SIGMA=0.05 (oxide)

NCORE = 1 (GPU), NELM = 500, VASP 6.4.3 GPU (CUDA/OpenACC)

POTCAR: Pd_pv (28Jan2005) + O (08Apr2002)

2026-06-09 | Pd/PdO/PdO₂ DMC Study | JBNU | Initial (POSCAR) structures