# G2 Slab Structure Report

Pd/PdO/PdO₂ DMC Formation Study — Clean Slab Structures

## Slab Structures

| S1: Pd(100) Metallic Pd, p(4×4), 4 layers | S2: PdO(101)/Pd(100) (√5×√5)R27° surface oxide on Pd(100) |
| --- | --- |
| S3: PdO(100) Bulk PdO, O-rich termination, 4×2 supercell | S4: PdO₂(110) Rutile-type PdO₂, stoichiometric termination |

## Slab Properties

| Surface | Oxidation | Atoms | Pd / O | Cell a×b (Å) | Layers | Fixed |
| --- | --- | --- | --- | --- | --- | --- |
| S1: Pd(100) | Pd⁰ | 80 | 80 / 0 | 11.0 × 11.0 | 5 | 32 |
| S2: PdO(101)/Pd(100) | Pd⁰/Pd²⁺ | 112 | 96 / 16 | 12.3 × 12.3 | 7 | 40 |
| S3: PdO(100) | Pd²⁺ | 128 | 64 / 64 | 12.2 × 10.8 | 8 | 32 |
| S4: PdO₂(110) | Pd⁴⁺ | 144 | 48 / 96 | 9.5 × 12.8 | 14 | 45 |

Generated: 2026-06-05  |  Pd=teal, O=coral  |  POV-Ray + ase3 texture