G2 Clean Slab Report — S1 / S2 / S3 / S4

Pd / PdO / PdO₂ DMC formation DFT study   |   2026-06-09   |   PBC images shown

All renders show periodic-image atoms within 2.5 Å of the cell boundary — so atoms that would otherwise be cut off at cell edges (and only re-appear on the opposite side via PBC) are explicitly drawn. Atom counts/stats below refer to the original simulation cell (without ghost duplicates).

## Guideline compliance (workplan line 28-29, T1.5)

| Slab | Fix policy | Atoms fixed | Vacuum | Status |
| --- | --- | --- | --- | --- |
| S1 | bottom 2 layers | 32/80 (40%) | 20.0 Å | ✓ |
| S2 | bottom 2 layers | 40/112 (36%) | 20.0 Å | ✓ [rebuilt] |
| S3 | bottom 2 layers | 32/128 (25%) | 20.1 Å | ✓ |
| S4 | bottom 4 sublayers (≈ 2 PdO₂ layers) | 42/144 (29%) | 20.0 Å | ✓ [rebuilt] |

Guideline: "Vacuum 20 Å, bottom 2 layers(또는 하단 30–40% 원자) 고정". S2 and S4 were rebuilt for this revision (previously vacuum 16.5 Å with ~50% fixed).

## Summary table

| Slab | Model | Atoms (Pd/O) | Cell a×b×c (Å) | Layers | Slab/Vac (Å) | Fixed/Free | Top Pd–O coord |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | Pd(100) | 80 (80/0) | 11.005 × 11.005 × 27.781 | 5 | 7.78 / 20.00 | 32/48 | {0: 32} |
| S2 | 1 ML PdO(101)/Pd(100) | 112 (96/16) | 12.303 × 12.303 × 29.165 | 7 | 9.17 / 20.00 | 40/72 | {2: 8, 4: 8} |
| S3 | PdO(100) | 128 (64/64) | 12.214 × 10.812 × 30.688 | 8 | 10.62 / 20.07 | 32/96 | {4: 24} |
| S4 | PdO₂(110) | 144 (48/96) | 9.532 × 12.848 × 32.103 | 12 | 12.10 / 20.00 | 42/102 | {5: 6, 6: 6} |

## Build & fix notes

S1 — Pd(100)  fcc Pd (a=3.8907) p(4×4), 5 layers, bottom 2 layers fixed. Vacuum 20 Å. CONVERGED (E=−434.408 eV).

S2 — 1 ML PdO(101)/Pd(100)  [REBUILT]  (√5×√5)R27°×2×2: 4 substrate Pd × 20 + 1 O–Pd–O sheet (16 Pd + 16 O). Strain ~1%, axis-aligned (R27° preserved internally, measured 26.6°). Bottom 2 substrate layers fixed (40/112=36%). Vacuum 20 Å. Matches Todorova 2003 / Kostelník 2007. Job 325.

S3 — PdO(100)  PdO tetragonal (100), 8 sublayers, bottom 2 fixed. Vacuum 20.1 Å. CONVERGED (E=−724.152 eV).

S4 — PdO₂(110)  [REBUILT]  Rutile PdO₂ (110) via pymatgen term=1 + rigid orthogonalization, 3×2 supercell. 12 sublayers, bottom 4 fixed (42/144=29%, ≈ 2 PdO₂ formula layers). Vacuum 20 Å. Top: 6× Pd_5c (cus) + 6× Pd_6c. Job 326.

## Fixed Atoms — color-coded side views (PBC images shown)

Grey = fixed (F F F); colored = free (T T T): Pd green, O red. Periodic image atoms (within 2.5 Å outside the cell along a, b) are drawn so atoms at the cell boundary appear complete instead of cut off.

S1  —  Pd(100)

S2  —  1 ML PdO(101)/Pd(100)

S3  —  PdO(100)

S4  —  PdO₂(110)

## Structures (PBC images, no lattice lines)

S1  —  Pd(100)

| Perspective | Top | Side |
| --- | --- | --- |

S2  —  1 ML PdO(101)/Pd(100)

| Perspective | Top | Side |
| --- | --- | --- |

S3  —  PdO(100)

| Perspective | Top | Side |
| --- | --- | --- |

S4  —  PdO₂(110)

| Perspective | Top | Side |
| --- | --- | --- |

## DFT status

| Slab | Job | Status | Notes |
| --- | --- | --- | --- |
| S1 | — | CONVERGED | E_tot = −434.408 eV |
| S2 | 325 | running | √5R27° guideline-compliant |
| S3 | — | CONVERGED | E_tot = −724.152 eV |
| S4 | 326 | queued | orthogonal PdO₂(110) guideline-compliant |

## Common INCAR

ENCUT = 520 eV   PREC = Accurate   LASPH = T   ADDGRID = T
EDIFF = 1e-6   EDIFFG = −0.03   NELM = 500   NSW = 300   IBRION = 2   ISIF = 2
ISPIN = 2   IVDW = 12 (D3 BJ)   ISMEAR = 0, SIGMA = 0.05
LDIPOL = T, IDIPOL = 3   KSPACING = 0.25   ISYM = 0
POTCAR: PAW_PBE O + PAW_PBE Pd_pv