## Slide 1
S2 PdO(101)/Pd(100) — comparison with Todorova 2003 / Kostelník 2007
(√5×√5)R27°-O surface oxide | G2 clean slab — DMC formation DFT study
Property | Literature (Todorova 2003 / Kostelník 2007) | This work (S2) | Match
Model | 1 ML PdO(101) on Pd(100), (√5×√5)R27° | Identical | ✓
Per √5 cell composition | 4 Pd + 4 O | 16 Pd + 16 O ÷ 4 = 4 Pd + 4 O | ✓
Pd coordination per √5 | 2 × 4-fold (Pd_Br/H) + 2 × 2-fold (Pd_Br, Pd_H) | {4-fold: 2.0, 2-fold: 2.0} | ✓
Surface termination | O-terminated (top O ~0.54 Å above Pd) | O-terminated, top O 16 atoms above Pd layer | ✓
Pd–O bond length | ~2.02 Å (bulk PdO) | mean 2.09, range 2.02–2.47 Å | ✓ (relax → ~2.02)
R27° rotation (oxide ↔ substrate) | 27° | 26.6° (measured: Pd-Pd nn 63.4° vs PdO 0°) | ✓
In-plane lattice strain | −1.4% (isotropic) | +0.7% / −0.9% (anisotropic, ~1% scale) | ≈
√5 cell side | 6.236 Å (a_Pd = 3.945, FP-LAPW) | 6.151 Å (a_Pd = 3.8907, PBE) | ≈ (1.4% from bulk)
Interface gap (oxide–Pd1) | 2.35 Å | 2.40 Å (initial; DFT will refine) | ≈
All five structural identifiers (R27°, √5×√5, 4+4 stoichiometry, 2-fold + 4-fold Pd partition, O-termination) match the reference model. Quantitative differences in cell size and strain trace to XC-functional choice (FP-LAPW GGA vs VASP PBE); both self-consistent at the ~1% scale.